## Slide 1: Module:1 Electronic Materials
vishal.vadgama@darshan.ac.in
+91 8866118980
Humanities and Science Department
Prof. Vishal S. Vadgama
Basic Science (Physics) (BSP)
GTU # 3110018

## Slide 2
Introduction to electronic materials
Electron theory of metals
Classical free electron theory
  Quantum free electron theory
  Band theory of solids or zone theory
  Types of electronic materials: conductor, Insulators, and
  semiconductors
  Kronig – Penny Model
  Energy band structure of a solid
  E – K Diagram
Topic

## Slide 3
Density of states
Effective mass of an electron
Fermi level and fermi function
Carrier concentration in metals
Phonon
Topic

## Slide 4
Introduction to
electronic materials

## Slide 5: Free electron theory

## Slide 6: Free electron theory
e-
e-
e-
A
Current: The flow of electric charge is called electric current.
One ampere current represents one coulomb of electric charge
One coulomb electric charge (q) = 6.24 × 1018 charge carriers (electrons)

## Slide 7: Terms related to electricity
Ohm’s law

## Slide 8: Terms related to electricity
Resistance: It is the opposition that a material offers to the flow of electric current.
We know,

## Slide 9: Terms related to electricity
Current density: The amount of electric current flowing per unit cross – sectional
area of a material.

## Slide 10: Terms related to electricity
Electric field: Voltage drop per unit length of a conductor.
Vf
Vi
L
We Know,
This equation is used when a moving charge goes
against the field (E).

## Slide 11: Terms related to electricity
Electric conductivity: The amount of electric current, a material can carry.
Ohm’s law
As we know,
Rate of charge flow across unit area (J)
Per unit potential field (E)

## Slide 12
Classification of
free electron theory
Classical free electron theory
Quantum free electron theory
Band theory
By
Drude-Lorentz Theory
By
Sommerfeld Theory
By
Bloch
Theory

## Slide 13: Basic terms involved in free electron theory
Drift velocity (Vd): The average velocity of charge carriers due to electric field.
Total Charge (Q) for an area (A) and length (L)
A
e-
e-
e-
L

## Slide 14: Basic terms involved in free electron theory
From, electrical conductivity
Mobility (𝛍): It is the drift velocity (Vd) acquired by electron (e-) per unit electric field.
Role of mobility in electrical conductivity:
Current density:
Drift velocity:
/
/
But,

## Slide 15: All equations

## Slide 16: Classical free electron theory
In 1900, Drude proposed free electron theory for metals using some basic
assumptions.
The valence electrons are free to move inside the metal just like gas molecules
inside a container.
This well arranged atoms or molecules
in any system are called lattice
e-
e-
e-
e-
e-
e-
e-
e-

## Slide 17: Assumptions/postulates of classical free electron theory
Metal structure consists positive ion core, with valence electrons moves
freely among these ion cores.
These valence electrons moves inside metal just like molecules in gas.
In the absence of electric field (E = 0), free electrons moves in random
directions and collide with each other.
e-
In the collisions, no loss of energy will observed because collisions are elastic.
When electric filed is applied (E ≠ 0), the free electrons are accelerated in direction opposite to
field.
Free electrons obey Maxwell-Boltzmann statistics.
E ≠ 0

## Slide 18: Basic terms involved in free electron theory
Relaxation time (τ): Time taken by an electron to reach equilibrium position from disturbed
position, in presence of electric field.
Mean free path (λ): The average distance travelled by electron between two successive collisions.
Mean collision time (τc): The average time between two successive collisions of electron.
e-
e-
e-
e-

## Slide 19: Expression for electrical conductivity
When electric field is applied, electrons experience a force
But,
As, electrons collision occurs during motion, the electrons will
get accelerated momentarily so, the drift velocity will be
Current density

## Slide 20: Expression for electrical conductivity
From, electrical conductivity
/
/
Expression for electrical conductivity

## Slide 21: Conductivity in terms of KBT (Ave. kinetic energy)
The relaxation time () in terms of mean free path (λ) and average thermal velocity is given by:
Kinetic energy of an electron based on kinetic theory
Here, KBT = Boltzmann constant
/
/
Using equation (8) & (7) in (6)
/
/
From equ. (9)

## Slide 22: Numerical
Q. A current of 5 A is passing through a metallic wire of cross sectional area 4×10-6
m2. If the density of the charge carriers in the wire is 5×1026 /m3, find the drift
speed of the electrons. (e = 1.6×10-19)
The relation between current (I) and drift velocity (Vd) of electron in wire of area (A) is
Where, n is the density of (free) electrons in the wire
I = 5 A
A = 4×10-6 m2
n = 5×1026 /m3
Vd = ?

## Slide 23: Numerical
Q. A conductor has an electron concentration of 5.9×1028 /m3. What density in the
conductor corresponds to a drift velocity of 0.625 m/sec. Calculate the mobility
of charge carriers. Given σ = 6.22×107 Ʊm-1.
Vd = 0.625 m/sec
J = ?
n = 5.9×1028 /m3
μ = ?
e = 1.6×10-19
(1.6×10-19)
(0.625)
J = 5.9×109 A/m2
μ = 6.588×10-3 m2/V·sec

## Slide 24: Numerical
Q. Calculate drift velocity of free electrons with a mobility of 3.5×10-3 m2 /V·sec in
copper for an electric field strength of 0.5 V/m.
μ = 3.5×10-3 m2/V·sec
E = 0.5 V/m
Vd = ?

## Slide 25: Expression for thermal conductivity (K)
It is defined as the rate of heat flow across a unit area of conductor per unit
temperature gradient.
ΔQ = rate of heat flow (thermal energy)
A = Cross-sectional area of conductor
A
B
λ
e-
e-
e-
Higher
Temp. (T)
Lower Temp.
(T-dT)
n = density of electrons
v = velocity of electrons

## Slide 26: Expression for thermal conductivity (K)
Average kinetic energy at A =
Average kinetic energy at B =
The excess energy carried by electrons
in traveling from point A to B
The electrons travel in all directions
crossing unit area from A to B
So, excess energy transferred from A to B
per unit area in unit time is:
Similarly, deficiency of energy from B to A
per unit time is:

## Slide 27: Expression for thermal conductivity (K)
The rate of heat flow can be defined as the
net energy transferred from A to B per unit
area per unit time:
We know thermal conductivity k is defined as:
Here, dx can be written as
mean free path (λ)
λ
/
/

## Slide 28: Wiedemann-Franz law
This law states that the ratio of thermal conductivity to electrical conductivity is directly
prepositional to the absolute temperature.
L = Lorentz number
By, taking ratio
/
/
/
/
/
/
Theoretical value of L: 1.12 × 10-8 WΩ/K2
Experimental value of L: 2.44 × 10-8 WΩ/K2
Theoretical and experimental values of L
doesn’t match with each other.
So, Assumption is wrong that all electrons
contributes in thermal conductivity.

## Slide 29: Success of free electron theory
It verifies ohm’s law.
It explains the thermal and electrical conductivities of a metal.
It helps to deduce Wiedemann – Franz law.
It explains optical properties of metals.

## Slide 30: Drawbacks of classical free electron theory
Theoratical value of specific heat and electronic specific heat of metal based is is not in
agreement with the experimental value (10-4 RT).
The classical free electron theory can’t explain electrical conductivity of insulators and
semiconductors.
According to classical theory, is constant at all temperature. But, this is not constant at
low temperature.
It failed to explain the superconductivity and magnetic susceptibility (χ).
The phenomena such as photoelectric effect, Compton effect and black body radiation can’t be
explained.
According to classical free electron theory, the electrical conductivity (σ) proportional to the
free electron density (n). But it failed to explain for different metals.

## Slide 31: Quantum free electron theory
After the failure of classical free electron theory for electrical, optical and thermal
properties of metal, modification became necessary.
The quantum statistical approach was introduced by Sommerfeld in 1928.
Here, the observed and predicted values of specific heat and paramagnetic
susceptibility of metal was corrected by quantum theory.
The classical approach was made by Maxwell-Boltzmann statistics while,
sommerfeld used Fermi-Dirac statistics for quantum approach.

## Slide 32: Quantum free electron theory
e-
X
Y
Z
e-
e-
e-
e-
K.E. = (↑)
P.E. = 0
ψ = (↑)
ψ = Probability of electrons
(Wave Function)

## Slide 33: Quantum free electron theory
e-
X
Y
Z
e-
e-
L
K.E. = 0
P.E. = (↑)
ψ = 0
ψ = Probability of electrons
(Wave Function)
X = 0
X = L
ψ = 0
ψ = 0
Boundary condition
At the boundary

## Slide 34: Quantum free electron theory
Each metal contains a very large number of electrons and these electrons can
move freely inside the metal.
Inside of the metal material uniform potential is applied:
  constantly moving electrons has only kinetic energy (K.E.) inside the metal
  while the potential energy (P.E.) is zero.
P.E. = 0 can be only possible when,
  Interaction of free electron with other electron and metallic core of the metal
  is negligible.

## Slide 35: Particle in one dimensional box
e-
X
Y
Z
K.E. ≠ 0 (↑)
P.E. = 0
ψ ≠ 0
L
X = 0
X = L
ψ = 0
ψ = 0
K.E. inside the material is not sufficient to overcome
metal boundary.
In quantum approach electrons moves in wave form and
wave nature of particle is given by Schrodinger.
Schrodinger wave equation for 3-dimension:
Schrodinger wave equation for 1-dimension:
E = total energy, V = potential energy, m = mass of electron
= modified planck’s constant

## Slide 36: Particle in one dimensional box
E = total energy,
V = potential energy,
m = mass of electron
In our case P.E. = 0
So, total energy (E) of the system
is because of only K.E.
To identify complementary function of :
Where, k = wave vector, A & B are constants
In order to find the values of A & B we can use two
boundary condition at X = 0 and X = L.
e-
X
Y
Z
ψ ≠ 0
L
X = 0
X = L
ψ = 0
ψ = 0
At X = 0 → ψ = 0
X = L → ψ = 0
Implying these two boundary condition values in
equation (3) for ψ

## Slide 37: Particle in one dimensional box
Putting this value in equation (3)
For, (1) X = 0 → ψ = 0 condition
For, (2) X = L → ψ = 0 condition
Here, B can’t be zero because than whole equation will be zero.
If ψ becomes zero than probability of having electron
Inside the metal becomes zero, which is not possible.
e-
X
Y
Z
ψ ≠ 0
L

## Slide 38: Particle in one dimensional box
Where, n = 0, 1, 2, 3…..
So, if we compare kL = nπ then:
By, comparing the values of k2
This problem can be satisfied by
taking sinkL zero instead of B.
Therefore, the wave function will be
valid only if:
/
/

## Slide 39: Particle in one dimensional box
According to this equation, electrons will
have nth level of energy (En) inside the metal.
E1
E2 = 4 E1
E3 = 9 E1
En = n2 E1
e-
e-
e-
e-
n = n
n = 3
n = 2
n = 1
Value of constant B in equ. 5 obtained by
applying the normalization condition to get
the value of wave function ψ.
Normalizing the wave function means you find
the exact form of probability (ψ) of the particle
which found somewhere in space is 1.
e-
X
Y
Z
ψ ≠ 0
L

## Slide 40: Particle in one dimensional box
Putting this value in equation (5)
This equation gives the value of probability
of electron in a confined system.
e-
X
Y
Z
ψ ≠ 0
L

## Slide 41: Particle in one dimensional box
Based on the value of energy we can apply probability function on a closed system.
E1
E2 = 4 E1
E3 = 9 E1
E4 = 16 E1
e-
e-
e-
e-
n = 4
n = 3
n = 2
n = 1
e-
X
Y
Z
L
X = 0
X = L
ψ = 0
ψ = 0
e-
e-
e-
e-
X = 0
X = L
ψ = 0
ψ = 0
X = L/2
ψ = 1
X = 0
X = L
X = L/2

## Slide 42: Particle in one dimensional box
X = 0
X = L
ψ = 0
ψ = 0
X = L/2
ψ = 1
X = 0
X = L
X = L/2

## Slide 43: Advantages of quantum free electron theory
It explains the specific heat of materials.
It explains Compton effect, photoelectric effect, blackbody radiation, Zeeman
effect.
It gives the correct mathematical expression for the thermal conductivity of
metals.
It explains the superconductivity.

## Slide 44: Drawbacks of quantum free electron theory
This theory fails to explain the positive value of Hall coefficients.
It failed to distinguish metal, semiconductor and insulator.
It failed to explain lower conductivities of divalent metals than monovalent
metals.

## Slide 45: Band Theory
(a) Formation of energy bands in solids:
In a single isolated atom, the electrons in each orbit have
definite energy associated with it.
In case of solids, the atoms are close to each other, so the
energy levels of outermost orbit electrons are affected by the
neighbouring atom.
When two single or isolated atoms are brought close to
each other, the outermost orbit electrons of the two atoms
interacts with each other.
  i.e. The electrons in the outermost orbit of one atom
  experiences an attractive force from the neighbouring
  atom nucleus.
e-
e-
e-
e-
e-
e-

## Slide 46: Band Theory
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-
e-

## Slide 47: Band Theory
e-
e-
e-
e-
e-
e-
e-
e-
As a result of this, the energy of electrons is no more the same, the energy levels are changed
to a value which is higher or lower than the original energy level.
The Pauli's exclusive principle allows each energy level to contain only two electrons.
“This grouping of different energy levels is called energy bands”.
The energy level of the inner orbit electrons are not much affected by presence of neighbouring
atoms.

## Slide 48: Band Theory
(b) Energy bands in solids:
The three important energy bands in solids.
Valence band:
  “The energy band formed by grouping the energy levels of valence electrons is called
  valence band”.
  Electrons in valence band have lower energy than electrons in conduction band.
  The electrons in valence band are loosely bound to nucleus of atom, they can be moved to
  conduction band by applying energy.
e-

## Slide 49: Band Theory
Forbidden band:
  “The energy gap that is present between the valence band and conduction band by
  separating the two energy band is called the forbidden band or forbidden gap.”
  Electrons can’t stay in this band as there is no allowed energy state in this gap.
  The energy associated with the forbidden gap is called the bandgap energy.
Conduction band:
  “The energy gap or band formed by grouping the energy levels of free electrons is called
  conduction band.”
  It is the uppermost band with free electrons, electrons have higher energy than electron is
  valence band.
  The band is completely empty for insulators and partially filled for conductors.
  The conduction band electrons are not bound to the nucleus of atom.

## Slide 50: Band Theory
Valence band
Conduction band
Forbidden band
Valence band
Conduction band
Valence band
Conduction band
Forbidden band

## Slide 51
Types of electronic materials: conductor, Insulators, and
semiconductors

## Slide 52: Types of electronic materials
Valence band
Conduction band
Forbidden gap
Insulators
Metals
Valence band
Conduction band
Semi-conductors
Valence band
Conduction band
Forbidden gap
e-
Lower energy state electron
e-
e-

## Slide 53: Types of electronic materials
Conductors:
  “ The materials which easily allow the flow of electric current are called conductors.”
    e.g. Copper, iron, silver, etc.
  The resistivity is of an order of 10-9 Ωm at room temperature.
  In a conductor, the conduction and valence band overlap each other as shown in figure.
  A small amount of energy provides enough energy for valence band electrons to move in
  conduction band.
Conduction band
Valence band
Overlapping
Energy (eV) →

## Slide 54: Types of electronic materials
Insulators:
  “ The materials which do not allow the flow of electric current
  through them are called insulators.”
  The valence band is completely filled with electrons. The
  forbidden energy gap is grater than 5 eV.
  The electrons in valence band can’t move to conduction as
  they are locked up between the atoms.
  It requires large amount of external energy to move the
  electrons to conduction band.
  The resistivity is of approx. 103 to 1017 Ωm at room temp.
Conduction band
Valence band
Energy (eV) →
Eg > 5 eV

## Slide 55: Types of electronic materials
Semi-conductors:
  “The materials which have electrical conductivity between that of
  conductors and insulators are called semiconductors.”
    e.g. Silicon, germanium
  The forbidden gap in semiconductors is very small (approx. 1eV).
  At low temp., valence band is completely filled with electrons and
  conduction band is completely empty as electrons don’t have
  sufficient energy to move in conduction band.
  As temp. increases, electrons gain energy and move to
  conduction band.
    Electrical conductivity increases with temperature.
  So, they have negative temperature coefficient of resistance.
Conduction band
Valence band
Energy (eV) →
Eg ≈ 1 eV

## Slide 56
Kronig – Penny Model

## Slide 57: Kroning Penney model
According to free electron theory:
  Homogeneous distribution of potential (voltage) electrons in metal.
  But it doesn’t explain it for semiconductor and insulators.
e-
From Band theory:
  Bloch suggested that: Potential of electrons varies periodically with lattice.
  Because inside the crystal, there is periodic arrangement positively charged
  ions, through which the electrons move.
+
+
+
+
+
+
+
+
+
+
+
+
-
+
+
+
+
e-
Here, variation in potential can be observed.

## Slide 58: Kroning Penney model
Kroning and Penney suggested:
+
+
+
+
e-
The potential of electron at the positive ion
site is zero and is maximum in between the
two (i.e. middle of two ions).
+
+
+
+
Potential (V = 0)
+
+
+
+
Potential (V = V0)
(V = 0)
(V = V0)
It was difficult to solve Schrodinger
equation with varying potential.
Kroning–Penney suggested that take
potential as shape of rectangular steps.
This model is called Kroning–Penney model.

## Slide 59: Kroning Penney model
I
II
0
a
-b
Potential (Vx)
V = V0
x
V = 0
e-

## Slide 60: Kroning Penney model
I
II
0
a
-b
Potential (Vx)
V = V0
The wave functions associated with this model can be calculated by solving Schrodinger
equations for the two regions I and II. (I = Potential well & II = Potential barrier)
Two consecutive potential wells are separated by a distance "b" (regions II) and the value of the
potential in each of these regions is "V0 ".
Therefore, potential of electron for the two regions can be expressed as v(x) = 0 for region-I and
v(x) = v0 for region-II.
x
V = 0

## Slide 61: Kroning Penney model
The Schrodinger’s equations are:
I
II
0
a
-b
V=V0
V=0
Now let us assume that the system is at room temperature and electrons do not acquire sufficient
thermal energy to escape from the crystal. Let us define two real quantities α and β such that:

## Slide 62: Kroning Penney model
I
II
0
a
-b
V=V0
V=0
The solution (according to Bloch theorem) that will be appropriate for both the regions (I & II) will
be of the form of a plane wave eikx modulated with a periodic function uk(x):
Where is propagation vector or wave vector
Using Bloch theorem and applying all boundary conditions for region (I & II) for continuity of the
wave function, solution of Schrodinger equation is obtained as:

## Slide 63: Graph of Kroning Penney model

## Slide 64: Kroning Penney model
I
II
0
a
-b
V=V0
V=0

## Slide 65: Kroning Penney model
The shaded portion of the wave shows the bands of allowed energy.
By increasing αa, allowed energy state for electron increases, thereby increase in band-width.
Increase in band-width leads to distance between electrons and total energy.

## Slide 66: Conclusion Kroning Penney model
Above equation shows the energy of free electron in conduction band.
Where is wave vector
According to De-Broglie’s theorem, we know,
P = particle momentum
h = Planck constant
λ = Wavelength
Energy band is broadened and it is continuous.

## Slide 67: Conclusion Kroning Penney model
/
/
The allowed states are
compressed to a line
spectrum.
If P is large, it results in
decrease of allowed energy
and increase if forbidden gap.

## Slide 68
Energy band structure of a solid

## Slide 69: Energy band structure of a solid
A crystal consists of large number of atoms arranged in a regular periodic structure. The extent of
energy level splits in the solids depends on the nearness of atoms.
Let us assume N identical atoms forms a crystal.
+
+
+
+
+
+
+
+
+
+
+
+
1s
2s
2p
3s
Energy States
2 N
2 N
6 N
2 N
e-
e-
e-
e-
E
Interatomic distance
E
Distance

## Slide 70: Energy band structure of a solid
The energy levels of the isolated atoms are shown in fig, All the N
atoms have identical sets of energy levels.
Electron fill the energy levels in each atom independently.
As the atoms approaches, a continuous increasing interaction
occurs between the atoms.
Each of the energy level splits into many distinct level and forms
energy bands, as shown in fig.
While occupying energy band, electrons starts from the lowest
energy level in the band and fill the levels one after another.
When 2N electron occupy the N levels available in the band, band is said to be completely filled.
In case on non availability of 2N electrons, energy band gets partially filled.
When there are no electrons to occupy the levels, the band remains vacant.
E
Distance
2 N
2 N
6 N
2 N
e-
e-
e-
e-

## Slide 71: Energy band structure of a solid
At room temperature, the kinetic energy of the electron is of the
order of kBT (≈ 0.026eV) which very large is compared to the
energy level separation in allowed band.
Electrons can easily move into higher vacant levels within the
allowed energy band either due to thermal energy or due to small
externally applied electric field.
The following two conditions are to be fulfilled for electrical
conduction to take place in solid.
There should be free electrons available in the solid.
Vacant energy levels should be available above the levels occupied by free electrons.
E
Distance
2 N
2 N
6 N
2 N
e-
e-
e-
e-

## Slide 72
E – K Diagram

## Slide 73: E – K diagram
“ An E – K diagram is a dispersion diagram that shows the relation ship between energy and
momentum of available states of electrons in a material.”
E
Valence band
Conduction band
Ec
Ev
Bottom value
Top value
E
k
e-
e-
e-
e-
Forbidden gap
(

## Slide 74: E – K diagram
E
Valence band
Conduction band
Ec
Ev
Bottom value
Top value
E
k
e-
e-
e-
From, the above diagram, we see the bottom value of conduction band corresponding to ‘Ec’ and
top value of valence band corresponds to ‘Ev’.
From, the E – K diagram, it can be seen that the holes which are closed to the top valence band
and electron which are close to the bottom of conduction band, participate in the transition
processes.

## Slide 75: E – K diagram
As all atoms are arranged periodically in lattice, we can say that semiconductors are crystalline
in nature.
+
+
+
+
a
a = interatomic distance
→ Varying potential
As per Bloch’s theorem, as the potential varies periodically, probability of finding an electron also
varies periodically.
Using this value in Schrodinger's equation:

## Slide 76: E – K diagram
Here, Schrodinger's equation gives periodic graph of ‘E’ versus ‘k’ for each allowed energy value.
E
k
0
The discrete energy value of k is in
the form of ……
The area between the to is
known as 1st Brillouin zone, and
between to is known as
2nd Brillouin zone

## Slide 77: E – K diagram
E
k
0
Here this periodic arrangement can
be understood by three zones.
  (1) Periodic Zone
  (2) Reduced Zone
  (3) Extended Zone
E
k

## Slide 78: E – K diagram
E
k
0
Extended Zone:
  Allowed Band
  Forbidden Band
  Allowed Band
  Forbidden Band
  Allowed Band
  Forbidden Band
  Allowed Band
  1st Brilliouin Zone

## Slide 79
Direct and Indirect bandgap semiconductors as per
E – K Diagram

## Slide 80: Direct bandgap semiconductor
E
k
Conduction Band
Valence Band
e-
e-
1 eV

## Slide 81: Direct bandgap semiconductor
E
k
Conduction Band
Valence Band
e-
Light

## Slide 82: Direct bandgap semiconductor
A direct band gap semi–conductor is the one in which maximum energy level of valence band
aligns with the minimum energy level of conduction band with respect to momentum.
  e.g. : GaAs
In a semi–conductor, the minimum energy state in conduction band and maximum energy state in
valance band is characterized by crystal momentum and wave vector ‘k’ (propagation constant).
In a direct bandgap semiconductor, the k-vectors are same for conduction band minima and
valence band maxima.
Whenever an electron from conduction band recombines with a hole from valence band, the
energy and momentum, both should be conserved.

## Slide 83: Direct bandgap semiconductor
The energy difference between conduction band and valence band is released in the form of a
photon.
The k-vectors of electron and hole are same. So, we say that momentum is also conserved.
We say the energy is conserved by emitting a photon.

## Slide 84: Indirect bandgap semiconductor
E
k
0
k
Conduction Band
Valence Band
E
Direct Bandgap
k
Conduction Band
Valence Band
E
e-
e-
Indirect Bandgap

## Slide 85: Indirect bandgap semiconductor
k
Conduction Band
Valence Band
E
e-
e-
An indirect bandgap semiconductor is the one in which maximum energy level of valence band
and minimum energy level of valence band and minimum energy level of conduction band are not
aligned with respect to momentum. e.g., Si, Ge.
In an indirect bandgap semiconductor, the k-vectors are different for conduction band minima and
valence band maxima.

## Slide 86: Indirect bandgap semiconductor
k
Conduction Band
Valence Band
E
e-
e-
In an indirect bandgap semiconductor, there is a difference in momentum. The recombination
process can occur only after the momentum align.
Due to crystal imperfections in certain semiconductors, the electron in the conduction band loses
energy and momentum at the same time.
The electron actually passes through an intermediate state and transfers
its momentum to the crystal lattice.
In this case, the energy is emitted in the
form of heat.
The transition is non-radiative in nature.

## Slide 87: Difference between direct and Indirect bandgap semiconductors
DBG semiconductor | IBG semiconductor
It is one in which maximum energy level of valence band aligns with the minimum energy level of conduction band with respect to momentum. | It is the one in which maximum energy level of valence band and minimum energy level of valence band and minimum energy level of conduction band are not aligned with respect to momentum.
In this direct recombination takes place with energy equal to the difference between energy of recombining particles. | In this due to a difference in momentum, first momentum is conserved by release of energy and only when the two momenta are aligned, recombination occurs.
The probability of radiative recombination is very high. | The probability of radiative recombination is almost negligible.
Efficiency factor is high. | Efficiency factor is low.
They are preferred for making optical devices like LED’s | Cannot be used to make optical device.

## Slide 88
Density of states

## Slide 89: Density of states
Density of states: The number of energy states per unit
volume of a metal.
It is use to calculate the number of charge carriers per unit
volume of any solid.
k
E
e-
e-
e-
e-
e-
e-
e-
number of energy states
unit volume
k + dk
k
E
E + dE
dE
Density of states N(E)dE is defined as the number of
available electron states per unit volume in an energy
interval (dE).

## Slide 90: Density of states
nx
nz
ny
Sphere called octant of n space
E
E+dE
dE
Δn
Let us consider a sphere of radius “n” in space with
quantum numbers nx, ny, nz.
The sphere is further divided into many shells represents a
particular combination of quantum numbers and represents
particular energy value.
n
Let us consider two energy values E and E+dE can be found
by finding the number of energy states between the shells
of radius n and n+ dn from the origin.
Since the quantum numbers are positive integers, n values
can be defined only in the positive octant of the n-space.
n+dn

## Slide 91: Density of states
The number of energy states within a sphere:
The number of available energy states within the sphere of radius
“n” due to one octant.
nx
nz
ny
E
E+dE
Δn
n
n+dn
Octant of n–space
Similarly the number of available energy states within the sphere of
radius n+dn corresponding energy.

## Slide 92: Density of states
nx
nz
ny
E
E+dE
Δn
n
n+dn
Octant of n–space
The number of available energy states between the shells of radius
n and n + dn (or) between the energy levels E and E + dE.
/
/
Since the higher powers of dn is very small, dn2 and dn3 terms can
be neglected.

## Slide 93: Density of states
We know that allowed energy values is
Differentiating equation (4) w.r.t ‘n’
Substituting (5) & (6) in equation (3)
/
/
/
/

## Slide 94: Density of states
Volume of the metal, V = a3
For unit volume of metal V = 1m3
/
/
Each electron energy level can accommodate two
electrons as per Pauli’s exclusion principle.
(Spin up and Spin down = 2 (e) × density of states).

## Slide 95
Effective mass of an electron

## Slide 96: Effective mass of electron
e-
+
+
+
+
+
+
+
+
Vacuum
e-
e-
e-
e-
e-
Mass of free electrons
Mass of electrons in solid
e = 9.1 × 10-31 kg
Experimentally measured values shows that for some solids the mass is larger,
while incase of other solids it is slightly smaller then free electron mass.
This experimentally determined electron mass is known as effective mass (m*).

## Slide 97: Effective mass of electron
e-
e-
+
+
+
+
+
+
+
+
Vacuum
e-
E
e-
e-
e-
e-
E
Consider mass of electron as
effective mass (m*).
Consider mass as per quantum
mechanical approach.
Then we can neglect internal
force in the crystal system,
where atoms having periodic
arrangement.
So, Periodic potential will be
applied on each electrons.

## Slide 98: Effective mass of electron
We see that same magnitude of electric field (E) is applied
to both electrons (In vacuum and inside the crystal), but the
electron accelerates at a different rate inside the crystal,
due to varying (periodic) potential inside the crystal.
e-
e-
+
+
+
+
+
+
+
+
Vacuum
e-
E
e-
e-
e-
e-
E
The electron mass is altered in this case due to the varying
potential.
“This altered mass is called effective mass of electron.”

## Slide 99: Effective mass of electron (m*)
According to De-Broglie hypothesis electron behaves like wave. Here, velocity acquired by electron
is known as group velocity (Vg):

## Slide 100: Effective mass of electron (m*)
Energy and Time are dependent
term, that’s why we exchange it.
According to De-Broglie’s theorem, we know,
differentiate above equ. w.r.t (t)
Substitute this value in equ. (2)

## Slide 101: Effective mass of electron (m*)
It is clear from the above equation that effective mass of an electron depends on E – K diagram.

## Slide 102
Fermi level and fermi function

## Slide 103: Fermi level
Fermi Level
E
Energy
Distance
Fermi level: “ The highest energy level which an electron can occupy at absolute zero (0 K) or
(– 273°C) temperature is called fermi level.”
Valence Band
Filled energy state
Conduction Band
Unoccupied levels
0 K
No, external energy is provided
Conductor / Metal
Semi–Conductor
Insulator
Fermi energy: “ The energy possessed by electrons in the fermi level at absolute zero
temperature is called fermi energy.”

## Slide 104: Fermi function
Fermi function is also known as Fermi – Dirac distribution function.
Fermi distribution function is used for half integer spin particles (fermions) like electrons, which
obey Pauli’s exclusive principle.
Statement: It is an expression for the distribution of electrons among the energy levels as a
function of temperature, the probability of finding an electron in a particular energy
state of energy E is given by:
f (E) | = Fermi function
Ef | = Fermi energy
T | = Absolute temperature (0 K)
kB | = Boltzmann constant (1.38 × 10-23 J/K)

## Slide 105: Fermi function
f (E) | = Fermi function
Ef | = Fermi energy
T | = Absolute temperature (0 K)
kB | = Boltzmann constant (1.38 × 10-23 J/K)
From above equation, we can say that a system is
characterized by its temperature and fermi energy (Ef).
For a filled energy level f(E) = 1 and for unfilled level f(E) = 0.
f(E) = 1
f(E) = 0

## Slide 106: Fermi function
Case I: At T = 0 K
At T = 0 K, Electron occupy lowest energy first, followed by next higher levels as per Pauli’s
exclusive principle.
1 S2
2 S2
2 P6
(a) At T = 0 K, E < Ef :
E
Ef
For energy level E, lying below Ef, (E – Ef)
makes negative value.
This implies that all energy levels below Ef are completely filled.

## Slide 107: Fermi function
(b) At T = 0 K, E > Ef :
E
Ef
For energy level E, lying above Ef, (E – Ef) makes positive value.
This implies that all energy levels above Ef are completely Vacant.
There is no possibility of electron occupying an energy level above Ef.

## Slide 108: Fermi function
E
Ef
Ef
f(E)
E
Valence Band
Conduction Band
0
0.5
1
E
Ef
f(E) = 1
f(E) = 0

## Slide 109: Fermi function
Case II: At T > 0 K
At room temperature, the probability starts reducing from 1 for values of E close to Ef, but larger
than Ef.
At T > 0 K, for E = Ef, exponential function becomes zero.
E
Ef

## Slide 110: Fermi function
Fermi Level
(T = 0 K)
f(E) = 0.5 implies that probability of occupancy of an electron is 50% at any
temperature above 0 K.
e-
e-
e-
e-
Ef
f(E)
E
Valence Band
Conduction Band
0
0.5
1
f(E) = 1
f(E) = 0
For E = Ef, the value of f(E) falls off to zero rapidly as shown in
the figure above.

## Slide 111: Fermi function
Case III: At T = very high temperature
At room temperature, it can be seen from the figure that the transition between completely filled
states and completely empty states is rather gradual than abrupt.
i.e. f(E) changes from 1 to 0 more gradually.
Ef
f(E)
E
Valence Band
Conduction Band
0
0.5
1
→ T = 300 K
→ T = 1500 K
→ T = 2500 K
As temperature (T) increases, electron may get an energy
of an order kBT and go to the higher vacant state.
Relation between fermi energy Ef, fermi velocity Vf
temperature Tf and mean free path λ is given by:

## Slide 112: Numericals
Q.1 Calculate the fermi velocity and mean free path for conduction electrons, given that its fermi
energy is 11.63 eV and relaxation time for electrons is 7.3 × 10–15 sec.
Ans.
Ef = 11.63 eV = 11.63 ×1.6 × 10–19 Joule
τ = 7.3 × 10–15 sec
Vf = ?
λ = ?

## Slide 113: Numericals
Q.2 Calculate the fermi energy and fermi temperature in a metal. The fermi velocity of electrons
in the metal is 0.86 × 106 m/sec.
Ans.
Vf = 0.86 × 106 m/sec
Ef = ?
Tf = ?

## Slide 114: Numericals
Q.3 Using fermi function, evaluate the temperature at which there is 1% probability that an
electron in a solid will have an energy 0.5 eV above Ef of 5 eV.
Ans.
E = 5.5 eV
Ef = 5 eV
f(E) = 1% = 0.01
T = ?
J
E
Ef
5 eV
5.5 eV
0.5

## Slide 115: Numericals

## Slide 116
Carrier concentration in metals

## Slide 117: Carrier concentration in metals
nx
nz
ny
E
E+dE
Δn
n
n+dn
Octant of n–space
The concentration of electrons, nc, having energy between E and
E + dE is given by

## Slide 118: Carrier concentration in metals
Calculation of fermi energy at T = 0 K
We will calculate the energy state in the order of increasing energy starting from E = 0 to the
highest filled state Ef, at T = 0 K
Fermi Level
(T = 0 K)
e-
e-
e-
e-
E = 0
FE = max.
At T = 0 K, f(E) = 1

## Slide 119: Carrier concentration in metals
/
/
Re–arranging the equ.1, we can define fermi energy
Multiply equ.2 with power 2/3

## Slide 120: Numericals
Q.1 Calculate the fermi energy for sodium. Given atomic weight 23 gm/mole and density of
sodium 0.97 gm/cm3.
Ans.
Atomic weight = 23 gm/mole = 0.023 Kg/mole = 23 × 10-3 Kg/mole
Density of sodium = 0.971 gm/cm3 = 0.971 × 103 Kg/m3
Ef = ?

## Slide 121: Numericals

## Slide 122
Phonon

## Slide 123: Phonon
A solid crystal consists of atoms bound into a specific three–dimensional pattern called lattice.
The atoms behaves as if they are connected by tiny springs and so their own thermal energy
(internal energy present in a system by virtue of temperature) or outside forces makes the lattice
vibrate.
This generates mechanical waves that carry heat and sound through the material.
A packet of these waves can travel throughout the crystal with definite energy and momentum.
These waves are treated as a particle called “phonons”.
+
+
+
+
+
+
+
+
+
+
+
+
E

## Slide 124: Phonon
Phonons acts like bosons, they can be created or destroyed in collisions.
Phonons exist with discrete amount of energy, given by
Where, = frequency of vibrations, h = plank constant
Phonons can carry heat and sound and they play a major role in determine heat capacities of solid
and liquids.

## Slide 125: Thank you